## Slide 1
Results
Methodology
Introduction
Modeling of basal and prismatic slip in 4H-SiC
Sheng’ou Lu, Binjie Xu, Lingling Xuan, Xiaodong Pi, Deren Yang, Xuefeng Han*
1. State Key Laboratory of Silicon and Advanced Semiconductor Materials & School of Materials Science and Engineering, Zhejiang University, China
2. Institute of Advanced Semiconductors, Hangzhou Global Scientific and Technological Innovation Center, Zhejiang University, China
E-mail: xuefenghan@zju.edu.cn
Governing equations
Alexander-Haasen model
Constitutive equation
Mechanical equilibrium equation
Vector system rotation
Conservation of energy equation
Simulation model
Calculation process
Stress tensor
Stress tensor
Elastic matrix
Strain tensor
Thermal expansion coefficient
Kronecker Symbol
Reference temperature
Heat source
Thermal conductivity
Emissivity
Stephen Boltzmann constant
Alexander-Haasen model : COMSOL implementation
Diameter effect
Stresses along growth direction
Temperature effect
Off-axis effect
Trend of basal and prismatic slip
Experimental comparison
Peter Wellmann, et al, physica status solidi (b), 2008
B. Gao and K. Kakimoto, Crystal Growth & Design, 2014
S. Hu, et al, Materials Science Forum. 2023
M. Dudley, et al, Journal of Electronic Materials, 2017
Source: Power SiC 2023, Yole Intelligence
Goal:
Diameter
Defect
Silicon carbide substrate
6-folds symmetry BPDs (4inch)
12-folds symmetry BPDs (6inch)
B. Xu, et al, Journal of Crystal Growth, 2023.
Two-dimensional axisymmetric global PVT model
S. o. Lu, et al, CrystEngComm, 2024
off-axis degree
N. Miyazaki, in Handbook of Crystal Growth, 2015
S. o. Lu, et al, submitted, 2024
Off-axis: COMSOL implementation
S. o. Lu, et al, submitted, 2024
6“
8“
Basal slip
Prismatic slip
S. o. Lu, et al, submitted, 2024
S. o. Lu, et al, CrystEngComm, 2024
S. o. Lu, et al, submitted, 2024
Three different temperature distributions
on-axis VS 4° off-axis
(a) vs (c)
Temperature difference
S. o. Lu, et al, submitted, 2024
A.Lara, et al, Ceramics International, 2012
M. Dudley, et al, Journal of Electronic Materials, 2017
0o
90o
6-fold
4-fold
S. o. Lu, et al, CrystEngComm, 2024
Off-angle effects on the dislocation distribution
CRSS
Basal slip 0.2 MPa
Prismatic slip 8 MPa
Critical slip stress
S. o. Lu, et al, submitted, 2024
Prismatic slip
(a) vs (b)
Absolute temperature
Prismatic slip stress
0o
90o
Basal
4-fold
Prismatic
6-fold
2-fold
12-fold
Excerpt from the Proceedings of the COMSOL Conference 2024 Shanghai